Experimental Evaluation of Calorific Value, Combustion Behavior, and Energy Efficiency of Rice Husk Briquettes for Agro-Processing

Abstract

This study explores the potential of rice husk briquettes (RHB) as an alternative fuel for cassava processing. Rice husks were compressed using a screw-press extrusion system, and their energy performance was evaluated by calorimetry and combustion testing. An Adobe SMART Stove was used for practical cassava-flaking tests. The briquettes had calorific values of 14.79–15.56 MJ/kg, operational temperatures of 615–710 °C and a reported combustion efficiency of 70%, compared with 16.2 MJ/kg, 850 °C and 80% for fuelwood. In cassava-flaking trials using 5 kg of sieved cassava per test, the reported processing time was 15 min for both fuels, while fuel consumption was 3 kg for the briquettes and 5 kg for fuelwood. Because the two fuels were tested in different stove arrangements, the fuel-consumption difference cannot be attributed to fuel properties alone. The results nevertheless demonstrate the technical potential of densified rice husk as a solid fuel for rural agro-processing and provide a basis for further controlled comparisons.

Keywords: Rice husk briquettes, Biomass energy, Calorific value, Combustion efficiency; Cassava processing, Agro-waste valorization; Sustainable fuel.

# INTRODUCTION

Cassava (Manihot esculenta) processing plays a crucial role in many tropical and subtropical regions, where the crop serves not only as a major staple food but also as an important source of income for rural households (Borku, 2025). The transformation of cassava roots into products such as cassava flakes (gari) involves several processing stages, including peeling, grating, dewatering, sieving, and roasting or flaking (Ngoualem Kégah and Ndjouenkeu, 2023; Clearinghouse, 2022). Among these steps, flaking is one of the most energy-demanding processes because it requires a steady and reliable heat supply to properly gelatinize and dry the cassava mash (Hans et al., 2023). In most rural communities, this heat is traditionally generated using biomass fuels such as firewood or charcoal.

However, the heavy reliance on firewood for cassava flaking presents serious environmental and socio-economic challenges. Continuous harvesting of fuelwood contributes to deforestation, biodiversity loss, and unsustainable land use (Girma and Shimeles, 2025). In addition, burning firewood releases greenhouse gases and particulate matter that contribute to climate change and air pollution (Łaska and Ige, 2023). The smoke produced during the flaking process also poses health risks to processors, especially women who are predominantly involved in small-scale cassava processing activities (Adeshina, 2024; Adeniyi et al., 2024; Agoh et al., 2024). These challenges highlight the need to explore cleaner, more sustainable energy alternatives for cassava processing (Iyiola, 2023).

In recent years, growing attention has been directed toward the use of agricultural residues as renewable biomass energy sources. One such residue is rice husk, a by-product of rice milling that accounts for about 20% of the harvested rice grain (Chieng and Kuan, 2022; Chavan et al., 2024). Large quantities of rice husk are generated globally each year and are often treated as waste or disposed of through open burning, which contributes to environmental pollution (Singh et al., 2021; Kesari and Jamal, 2017). Nevertheless, rice husk contains considerable energy potential and can be converted into briquettes through densification processes, thereby improving its fuel quality and usability (Sithole et al., 2023; Vijaya et al., 2025; Yunusa et al., 2025).

Rice husk briquettes (RHB) are compacted biomass fuels with higher energy density, improved combustion characteristics, and easier handling compared to loose agricultural residues (Ali et al., 2024; Yank et al., 2016). Because they are renewable and widely available, RHB have gained attention as a promising alternative fuel for thermal applications in agro-processing industries (Kapoor and Sillanpää, 2025; Vishnu Priyan et al., 2024). Their use in cassava flaking could reduce dependence on firewood, lower environmental impacts, and promote more sustainable energy use within rural agricultural value chains (Asante, 2022; Tshimungu et al., 2026).

The use of different biomass fuels in food processing applications offers advantages such as renewability and environmental sustainability (Kataya et al., 2023; Gheidan et al., 2021). However, challenges related to fuel properties characterization and potential competition with food production need to be addressed to ensure the efficient and sustainable integration of biomass energy into food processing operations (Khalil and DanielRos, 2025; Mignogna et al., 2024).

Therefore, this study focuses on producing briquettes from rice husk and evaluating their thermal performance by determining the heat energy output generated during combustion. The study also examines the feasibility of integrating rice husk briquettes as an alternative energy source for cassava flaking. By converting agricultural waste into a useful energy resource, this research aims to improve energy efficiency, promote sustainable cassava processing, and contribute to environmental protection and rural economic development.

# METHODOLOGY

## Experimental Design and Study Location

This study used an experimental approach to evaluate the performance of rice husk briquettes as an alternative fuel for cassava processing. Rice husk was obtained from a local rice-milling centre in Wukari, Taraba State, Nigeria. The cassava used for the processing trials was the TMS 30572 variety, harvested at approximately 9 months of age. The rice husk was manually sorted to remove stones, foreign matter and other visible impurities, then spread in a clean open area and sun-dried for three days. Moisture loss during preparation was monitored gravimetrically. For oven-based moisture determination, representative samples were dried at 105 °C to constant mass. The dried samples were allowed to cool for 24 h before weighing and testing. Mass was measured with a digital analytical balance (Mettler Toledo, 0.0001 g sensitivity).

## Rice Husk Briquette Production

Briquette production was carried out using a screw-press extruder-type briquetting machine (Figure 1) powered by a 7.5 hp, 380 V electric motor operating at about 970 rpm and fitted with three 5 kW heating coils. The heating coils maintained die-barrel temperatures between 300 and 330 °C, which softened the natural lignin in the rice husk and promoted particle binding as the material passed through the die. The resulting briquettes were produced in hexagonal form, cooled for 24hrs and stored in a ventilated, moisture-free room.

Figure 1: Screw press extruder-type briquetting machine used for rice husk briquette production.

## Calorific Value and Combustion Monitoring

Calorific values were determined with an IKA C 2000 oxygen bomb calorimeter using dried samples and the instrument's combustion-calorimetry procedure. Operational temperature, DC current and burning time were monitored separately in a forced-air combustion arrangement consisting of a DC power supply, an ammeter, a blower and a K-type thermocouple. The ammeter recorded the DC current supplied to the blower, while a stopwatch was used to record burning time.

## Adobe SMART Stove and Cassava-Flaking Test

An Adobe SMART Stove (Figure 2) was designed and built specifically for this research. The stove had a double-wall structure of locally produced adobe bricks, with outer and inner footprints of approximately 1.12 m × 1.12 m and 0.97 m × 0.97 m, respectively, separated by a 12.7 cm gap filled with a dry clay–sand mixture to trap heat and reduce heat loss. The inner combustion chamber was lined with galvanised metal sheeting and contained a mild-steel grate, a removable ash tray and a metal chimney, and a cast-iron plate served as the cooking surface. A 12 V DC fan installed at the air inlet supplied forced air to the combustion chamber and was powered by a photovoltaic system to keep the entire system running on renewable energy. The fan speed could be adjusted using a variable resistor, giving control over the burning rate and cooking temperature.

Figure 2: The completed Adobe SMART Stove, showing the double-wall adobe structure, the DC fan at the air inlet and the chimney.

To evaluate performance under practical processing conditions, fresh cassava roots of the TMS 30572 variety were weighed, peeled, washed with water from a solar-powered water pump, grated, dewatered and sieved to obtain a uniform mash. Each fuel test used 5 kg of sieved cassava. For the rice husk briquette treatment, the cassava was fried into flakes in the Adobe SMART Stove. For comparison, fuelwood was tested in an open setup representing the traditional processing arrangement. Fuel mass consumed, processing time and final product mass were recorded for each test. Each experimental condition was repeated five times. Data were entered and analysed using IBM SPSS Statistics, with descriptive statistics reported as mean ± standard deviation. Where inferential comparisons were appropriate, statistical significance was assessed at P < 0.05.

# RESULTS AND DISCUSSION

Production of the rice husk briquettes, determination of their heat energy output, and comparison of their energy efficiency with traditional fuelwood in cassava processing were carried out as described in the Methodology section. Data were collected on energy input, processing time and product quantity to assess the benefits of using rice husk briquettes in place of traditional fuel.

## Physical Characteristics of the Rice Husk Briquettes

The results of the briquette production are presented in Table 1.

Table 1:  Rice Husk Briquette Production

| Parameter | Sample |
| --- | --- |
| Initial rice husk weight(Kg) | 1.25 |
| Pressure applied Nm-2) | 6×109Nm-2 |
| Briquette weight (Kg) | 1.0 |

The results presented in Table 1 show the mass conversion of 1.25 kg of rice husk into briquettes at an applied pressure of 6x109 Nm-2. The initial weight of rice husk used in the experiment was 1.25 kg.

The applied pressure gave a briquette weight of 1.0 kg. This shows that approximately 80% (1.0/1.25 × 100%) of the initial rice husk weight was retained in the briquette form, a mass loss of about 20%. The application of pressure is necessary for the process as it compacts the loose rice husk particles into solid briquettes, and the magnitude of pressure required depends on the cohesiveness and density of the material. The mass loss is attributed to moisture loss during heating and to fine particles that did not compact effectively, which is consistent with the literature (Saeed et al., 2021). Because the husk was sun-dried and not oven-dried, the loss reflects moisture and fines together and is not an absolute moisture content.

## Calorific Value and Combustion Behaviour

The heat energy output of the rice husk briquettes is shown in Table 2, which lists the calorific value, burning time, operational temperature and the DC current supplied to the blower that regulated the air supply to the combustion chamber.

Table 2: Heat Energy Output Determination of Rice Husk Briquettes (five repeated experimental conditions)

| Rice Husk Briquettes (kg) | Calorific Value (MJ/kg) | Burning Time (min) | Operational Temperature (°C) | Current(I) DC (A) |
| --- | --- | --- | --- | --- |
| 5 | 14.79 | 15 ± 2 | 615 ± 60 | 1.5 |
| 5 | 14.83 | 13 ± 2 | 630 ± 62 | 1.8 |
| 5 | 15.10 | 13 ± 2 | 655 ± 65 | 2.3 |
| 5 | 15.12 | 12 ± 2 | 682 ± 68 | 2.5 |
| 5 | 15.56 | 12 ± 2 | 710 ± 70 | 2.7 |

Table 2 presents the calorific values of the rice husk briquettes, which ranged from 14.79 to 15.56 MJ/kg, with a small increase across the trials. The calorific value was determined by bomb calorimetry, whereas the operational temperature and DC current were recorded in a separate forced-air combustion arrangement; the trend of calorific value with these operating parameters is therefore an association and should not be taken to mean that the operating conditions changed the intrinsic energy content of the fuel. The values are lower than, but of the same order as, those reported for rice husk briquettes in previous studies (Yank et al., 2016; Saeed et al., 2021). The highest value obtained (15.56 MJ/kg) is about 12% lower than the 17.688 MJ/kg reported by Saeed et al. (2021) for rice husk briquettes produced at controlled moisture content with a kraft lignin binder. Such differences can be attributed to feedstock composition, moisture condition, binder and production conditions, as well as the fixed carbon and volatile matter content of the fuel, since the calorific value of a solid fuel depends largely on its carbon content and proximate composition.

As observed in Table 2, the burning time decreased slightly from 15 ± 2 minutes to 12 ± 2 minutes as the operational temperature and the DC current supplied to the blower increased. This suggests that a higher air supply and temperature accelerate the combustion process and shorten the burning time. However, the burning times of adjacent trials overlap within their stated uncertainty (± 2 min), so this trend should be regarded as indicative.

Figure 3, shows an inverse relationship between the calorific value of the briquettes and their burning time: briquettes with higher calorific values burned for a shorter time. The present measurements do not independently establish the fuel-property mechanism responsible for this relationship. A shorter burning time is often associated with a higher volatile matter content, because volatiles such as tars and other hydrocarbons are combustible and have a low flash point. Ignition time was not measured in this study, but according to Sani et al. (2019), briquettes with a short ignition time raise safety concerns during storage because the risk of ignition and fire is increased; caution must therefore be taken to keep briquettes free from sparks and extreme heat. The longest burning time, 15 ± 2 minutes, may be influenced by factors such as the duration of initial combustion, adhesion between briquette particles, and ventilation during and after combustion.

Figure 3. Relationship between calorific value and burning time of rice husk briquettes

Table 2 shows a progressive increase in operational temperature from 615 ± 60 °C to 710 ± 70 °C. The mean operational temperature was approximately 658 °C. The temperature increase coincided with an increase in DC current from 1.5 to 2.7 A. This is consistent with the operation of the forced-air system: increasing the electrical drive to the blower increased air movement through the combustion chamber, which supported combustion and raised the measured temperature. Because airflow rate was not measured directly, the DC current should be regarded as a control indicator rather than a direct airflow measurement. A K-type thermocouple was used for temperature measurement.

From Table 2, the smallest measured calorific value was 14.79 MJ/kg, while the highest was 15.56 MJ/kg. These values were obtained from the bomb-calorimetry measurements and should be interpreted primarily as fuel-property measurements rather than consequences of the operating temperature. Differences among briquette samples may reflect variation in feedstock composition, moisture condition and densification history; however, these factors were not independently quantified in the present experiment. Figure 4, further shows that increasing DC current was associated with increasing operational temperature because the blower supplied progressively stronger forced air to the combustion chamber. The trend therefore supports the use of blower control as an operational means of regulating combustion intensity within the tested range.

Figure 4. Relationship between operational temperature and DC current supplied to the blower

## Comparative Thermal Performance of Rice Husk Briquettes and Fuelwood

Table 3:  Heat Energy Output Determination between fuelwood and rice husk briquettes

| Parameter | Rice Husk Briquette | Fuelwood |
| --- | --- | --- |
| Sample Weight (kg) | 1 | 1 |
| Calorific Value (MJ/kg) | 14.8 | 16.2 |
| Burning Time (min) | 15 | 15 |
| Maximum Temperature Achieved (°C) | 780 | 850 |
| Combustion Efficiency (%) | 70 | 80 |

Table 3 compares the heat energy output of fuelwood and rice husk briquettes, which allows the performance of the two energy sources to be evaluated. Fuelwood showed a slightly higher calorific value (16.2 MJ/kg) than the rice husk briquettes (14.8 MJ/kg), indicating that it can release more energy per unit mass; however, the difference is modest (about 9%), which suggests that rice husk briquettes are a competitive alternative. Both fuels had an equal burning time of 15 minutes, showing similar combustion durations under comparable conditions, so the briquettes can match fuelwood in sustaining heat over time. The rice husk briquettes attained a maximum temperature of 780 °C while fuelwood reached 850 °C, so fuelwood gave a slightly higher heat intensity; nevertheless, the briquettes reached temperatures sufficient for most heating applications, including cooking. The combustion efficiency of the rice husk briquettes was 70%, compared with 80% for fuelwood. The higher efficiency of fuelwood may be related to its composition and higher energy density. However, the efficiency of the rice husk briquettes (70%) is encouraging, considering that they are a renewable and environmentally friendly by-product.

Table 4: Cassava Processing Comparison

| Parameter | Rice Husk Briquette | Fuelwood |
| --- | --- | --- |
| Initial Cassava Weight (kg) after sieving | 5 | 5 |
| Processing Time (min) (i.e frying time) | 15 | 15 |
| Fuel Consumption (kg) | 3 | 5 |
| Final Product Weight (kg) | Not available | Not available |

Table 4 compares the performance of rice husk briquettes and fuelwood in cassava flaking. Both methods used 5 kg of sieved cassava per test. The reported frying time was 15 minutes for both fuels. Rice husk briquettes consumed 3 kg of fuel compared with 5 kg for fuelwood, a 40% lower fuel consumption by mass. This difference should not be interpreted as a 40% improvement in energy efficiency because the fuels have different calorific values and were tested in different stove arrangements (the Adobe SMART Stove for briquettes and an open fuelwood setup). The final-product mass is not recalculated here because the available source data in the manuscript were based on the earlier 2 kg cassava test and therefore cannot be transferred to the revised 5 kg test without the original raw measurements.

# CONCLUSION

The findings indicate that rice husk briquettes can provide a practical alternative fuel for cassava processing under the conditions tested. The briquettes had calorific values of 14.79–15.56 MJ/kg and produced operational temperatures of 615–710 °C in the forced-air combustion system. In the cassava-flaking trial, the briquettes and fuelwood produced the same reported processing time of 15 min, while the reported fuel consumption was 3 kg and 5 kg, respectively. Because the two fuels were tested in different stove arrangements, the observed fuel-consumption difference should not be interpreted as a fuel-only efficiency advantage. Nevertheless, the results demonstrate the technical potential of rice husk densification for converting an agricultural residue into a usable solid fuel for rural agro-processing.

Declaration of AI Use

This manuscript was prepared through the intellectual contributions of the author(s) to the study design, data analysis, interpretation of results, and scholarly content. Grammarly and ChatGPT were used solely to assist with grammatical refinement and reference formatting during manuscript revision. The author(s) accept full responsibility for the accuracy, integrity, and final content of the manuscript.

# References

Adeniyi, V., Akangbe, J., Kolawole, A., & Okonta, O. (2024). Comparison of occupational and

environmental health hazards associated with the use of improved and conventional cassava processing technologies in Nigeria. In 2024 International Conference on Science, Engineering and Business for Driving Sustainable Development Goals (SEB4SDG). https://doi.org/10.1109/SEB4SDG60871.2024.10630379

Adeshina, O. O. (2024). Exposure to air pollution and lung function among cassava grits (Gari)

processors in Ghana (Doctoral dissertation, London School of Hygiene & Tropical

Medicine).

Agoh, E. C., Ogwu, M. C., Chukwuemeka, O. S., & Ekeledo, P. I. (2024). Environmental and

human health effects of cassava processing and processing waste. In Sustainable Cassava (pp. 203–219). Academic Press. https://doi.org/10.1016/B978-0-443-21747-0.00001-1

human health effects of cassava processing and processing waste. In Sustainable Cassava (pp. 203-219). Academic Press.

Ali, A., Kumari, M., Manisha, Tiwari, S., Kumar, M., Chhabra, D., & Sahdev, R. K. (2024). Insight

into the biomass-based briquette generation from agro-residues: challenges, perspectives, and innovations. BioEnergy Research, 17(2), 816-856

Asante, E. (2022). Environmentally sustainable cassava processing in Ghana: Trade-offs between

the different United Nations Sustainable Development Goals (Doctoral dissertation).

Benti, N. E., Gurmesa, G. S., Argaw, T., Aneseyee, A. B., Gunta, S., Kassahun, G. B., Aga, G. S.,

& Asfaw, A. A. (2021). The current status, challenges and prospects of using biomass energy in Ethiopia. Biotechnology for Biofuels, 14(1), 209. https://doi.org/10.1186/s13068-021-02060-3

Borku, A. W. (2025). Cassava (Manihot esculenta Crantz): Its nutritional composition insights for

future research and development in Ethiopia. Discover Sustainability, 6(1), 404. https://doi.org/10.1007/s43621-025-00996-2

Chavan, S., Mitra, D., & Ray, A. (2024). Harnessing rice husks: Bioethanol production for sustainable future. Current Research in Microbial Sciences, 7, 100298. https://doi.org/10.1016/j.crmicr.2024.100298

Chieng, S., & Kuan, S. H. (2022). Harnessing bioenergy and high value-added products from rice residues: A review. Biomass Conversion and Biorefinery, 12, 3547–3571. https://doi.org/10.1007/s13399-020-01238-1

Gheidan, A. A., Wahid, M. A., Munir, F. A., & Opia, A. C. (2021). Feasibility study of bio-fuel

as a sustainable product of biomass: an overview of its fundamentals, application and environmental impact. J. Adv. Res. Fluid Mech. Therm. Sci, 88(2), 106-122.

Girma, G. A., & Shimeles, A. (2025). Woodfuel production and its implication in driving deforestation in the drylands of Ethiopia. Indonesian Green Technology Journal, 14(2). https://doi.org/10.21776/ub.igtj.2025.014.02.05

Hans, M., Lugani, Y., Chandel, A. K., Rai, R., & Kumar, S. (2023). Production of first-and second-

generation ethanol for use in alcohol-based hand sanitizers and disinfectants in   India. Biomass conversion and biorefinery, 13(9), 7423-7440.

Iyiola, a. T. (2023). Occurrence and health implications of fungi and aflatoxins from cassava flakes

(garri) collected from selected agro-ecological zones (aezs) in nigeria (doctoral dissertation).

Kapoor, R. T., & Sillanpää, M. (Eds.). (2025). Biomass-based Green Technology for Circular

Economy. CRC Press.

Kataya, G., Cornu, D., Bechelany, M., Hijazi, A., & Issa, M. (2023). Biomass waste conversion

technologies and its application for sustainable environmental development—a review.

Agronomy, 13(11), 2833. https://doi.org/10.3390/agronomy13112833

Khalil, I. A., & DanielRos, M. (2025). Biomass Energy: Pathways, Potentials, and Challenges for

a Sustainable Energy Future. Energy Conversions.

Kesari, K. K., & Jamal, Q. M. S. (2017). Review processing, properties and applications of

agricultural solid waste: effect of an open burning in environmental toxicology. Perspectives in environmental toxicology, 161-181.

Łaska, G., & Ige, A. R. (2023). A review: Assessment of domestic solid fuel sources in

Nigeria. Energies, 16(12), 4722. https://doi.org/10.3390/en16124722

Mignogna, D., Szabó, M., Ceci, P., & Avino, P. (2024). Biomass energy and biofuels: Perspective, potentials, potentials, and challenges in the energy transition. Sustainability, 16(16), 7036.https://doi.org/10.3390/su16167036

Ngoualem Kégah, F., & Ndjouenkeu, R. (2023). Gari, a cassava (Manihot esculenta Crantz) derived product: review on its quality and their determinants. Journal of Food Quality, 2023(1), 7238309. https://doi.org/10.1155/2023/7238309

Ondari, B. O., Kimutai, S., & Mukubwa, E. (2025). Combustion characteristics of briquettes of different feed-stock of agricultural wastes: A review. International Journal of Research and Innovation in Applied Science, 10(6), 1654–1662. https://doi.org/10.51584/IJRIAS.2025.100600124

Saeed, A. A. H., Harun, N., Bilad, M. R., Afzal, M. T., Parvez, A. M., Roslan, F. A. S., Abdul Rahim, S., Vinayagam, V. D., & Afolabi, H. K. (2021). Moisture content impact on properties of briquette produced from rice husk waste. Sustainability, 13(6), 3069. https://doi.org/10.3390/su13063069

Singh, G., Gupta, M. K., Chaurasiya, S., Sharma, V. S., & Pimenov, D. Y. (2021). Rice straw burning: A review on its global prevalence and the sustainable alternatives for its effective mitigation. Environmental Science and Pollution Research, 28, 32125–32155. https://doi.org/10.1007/s11356-021-13707-1

Sithole, T., Pahla, G., Mashifana, T., Mamvura, T., Dragoi, E. N., Saravanan, A., & Sadeghifar, H. (2023). A review of the combined torrefaction and densification technology as a source of renewable energy. Alexandria Engineering Journal, 82, 330–341. https://doi.org/10.1016/j.aej.2023.09.080

Suryaningsih, S., Nurhilal, O., Yuliah, Y., & Salsabila, E. P. (2018). Fabrication and Characterization of Rice Husk Charcoal Bio Briquettes. https://doi.org/10.1063/1.5021237

TAAT Clearinghouse. (2022). Cassava processing technology toolkit catalogue (Clearinghouse Technical Report Series 013). Gates Open Research, 6, Article 92. https://doi.org/10.21955/gatesopenres.1116887.1

Tshimungu, T. B., Isah, M. E., & Ishii, K. (2026). Harnessing cassava-based ethanol for rural communities: A conditional circular pathway to reduce biomass dependence in rural Congo. Energy for Sustainable Development, 93, 101982. https://doi.org/10.1016/j.esd.2026.101982

Vijaya, Idrishi, R., Singh, S., & Islam, M. (2025). Processing of rice husk and its applications. In Rice Husk Biomass: Processing, Properties and Applications (pp. 1–26). Springer. https://doi.org/10.1007/978-981-96-1082-2_1

Vishnu Priyan, V., Sathasivam, J., & Kumar, A. (2024). Valorisation of agricultural waste into a low-cost adsorbent: Perspective of reutilization. In Agricultural Waste to Value-Added Products (pp. 125–149). Springer. https://doi.org/10.1007/978-981-97-2535-9_6

Yank, A., Ngadi, M., & Kok, R. (2016). Physical properties of rice husk and bran briquettes under low pressure densification for rural applications. Biomass and Bioenergy, 84, 22–30. https://doi.org/10.1016/j.biombioe.2015.09.015

Yunusa, S. U., Mensah, E., Narra, S., Saleh, A., & Preko, K. (2025). Strategies for improving the quality of low-pressured rice husk briquette: A mini-review. In M. M. Narra & S. Narra (Eds.), African green transition through innovative pathways (pp. 65–80). Springer. https://doi.org/10.1007/978-3-031-87043-9_4